Title: Survival of glass ionomer restorations placed in primary molars using atraumatic restorative treatment (ART) and conventional cavity preparations: 2-year results

Author(s): Yu C, Gao XJ, Deng DM, Yip HK, Smales RJ

Source: INTERNATIONAL DENTAL JOURNAL 54 (1): 42-46 FEB 2004

Document Type: Article

Language: English

Cited References: 19      Times Cited: 1

Abstract: Objective: To compare the survival of glass ionomer cement (GIC) restorations placed in a dental clinic setting using both the atraumatic restorative treatment (ART) approach with hand instruments, and conventional cavity preparation with rotary instruments. Method and Materials: Two encapsulated high-strength conventional GICs (Fuji IX GP, Ketac-Molar Aplicap) were placed in 82 Class I and 53 Class 11 preparations and one encapsulated non-gamma 2 amalgam alloy (GK-amalgam) was placed in 32 Class I preparations, in the primary molars of 60 Chinese children with a mean age of 7.40 +/- 1.24 (SD) years. Thus, 9 treatment groups were formed. Results: After two years, there were no significant survival differences found among 7 of the 9 treatment groups (p = 0.99). However, two groups comprising Fuji IX GP and Ketac-Molar Aplicap placed in Class II cavities prepared using the ART approach showed significantly lower restoration survivals (p < 0.001). Only 3 of the 72 initially sealed fissures adjacent to the restorations appeared to retain any GIC material. Conclusions: in a clinic setting, both the ART hand instrument and conventional rota instrument methods were equally suitable for high Class I restoration survival, but not for Class II restoration survival where the conventional cavity preparation method was preferable.

Author Keywords: atraumatic restorative treatment; glass ionomer cement; primaty teeth

KeyWords Plus: SEALANTS

Addresses: Yip HK (reprint author), Prince Philip Dent Hosp, 34 Hosp Rd, Hong Kong, Hong Kong Peoples R China
Prince Philip Dent Hosp, Hong Kong, Hong Kong Peoples R China

E-mail Addresses: hkyip@hkusua.hku.hk

Publisher: F D I WORLD DENTAL PRESS LTD, 5 BATTERY GREEN RD, LOWESTOFT NR32 1 DE, SUFFOLK, ENGLAND

Subject Category: DENTISTRY, ORAL SURGERY & MEDICINE

IDS Number: 909AM

ISSN: 0020-6539